## Slide 1: BLIP operations 03-15-11
Status – off
  BLIP weekly average beam reduced to 97.0µA purposely. Operations decreased to 158.4 hours due to Linac maintenance.
  A broader Gaussian profile was achieved and another trial with a Ga target began 3/8 at slightly reduced intensity. No failure so far.
  Isotope production of Sr-82 and irradiation LBNE targets downstream of the isotope targets continues. Research irradiation for Cu-67was completed 3/8.
Operations issues
  Target drive system failure today
    Preliminary diagnosis is that the sprocket on drive #2 is slipping on the motor shaft. Repair requires access to the contaminated motor housing on top of the hot cell. A RWP is being prepared.
  Investigation of cause of Ga targets leaks continues.
    We are investigating an alternate target design involving vapor deposition of either rhenium or alumina as a protective layer on the Nb cladding interior. Test pieces are being fabricated.

## Slide 2
Chart: To Date Accum. uA-hrs